SECTION 514-0001 – ANTI-GRAFFITI COATING

514-0001.01  DESCRIPTION. This work shall consist of applying an anti-graffiti coating system for the sealing and protection of concrete surfaces as indicated in the Plans and as directed by the Engineer.

514-0001.02  MATERIALS. Anti-Graffiti Coating shall meet the requirements of ASTM D6578: Graffiti Resistance Class 1 and ASTM D7089: Effectiveness of anti-graffiti coating by pressure washing: Cleanability Level 1.

Materials and coating(s) systems furnished under this Section shall conform to the manufacturer’s specifications.

Coatings must not react deleteriously with above grade concrete, concrete block, exposed aggregate concrete, brick, stonework, painted steel, or aluminum substrates. Coatings shall dry as a matte or satin finish and must cure to be clear/transparent.

The consistency must be such that the coating can be satisfactorily applied by roller, or brush at atmospheric and material temperature above 50°F without thinning. When properly applied to vertical surfaces, the coating must remain uniform during the required curing period and must not sag, disintegrate, check, peel, or crack.

The coating shall have the capability of having all types of paint and graffiti material removed without damaging the surfaces to which the coating is applied. Removal of graffiti shall not result in “shadowing” of the base surface upon removal of graffiti.

Coating must allow for removal of graffiti with a low-pressure water wash. Pressure wash requirements must not exceed 500 psi, and the cured coating must not be damaged by a 1,700-psi pressure wash. Must be washable with water an ambient temperature of 50°F or higher.

All other materials shall be in accordance with the Plans and Specifications and shall be approved by the Engineer prior to use.

514.0001.03 SUBMITTALS. Four weeks prior to beginning the work, the Contractor shall provide Product Data Sheets, along with Material Safety Data Sheets for the coating products including thinners and cleaning agents.

514-0001.04  APPLICATION. All surfaces that are to be treated shall be at least 30 days old and as required by the coating manufacturer. These surfaces shall also be cleaned as required by the manufacturer to remove any latency, dirt, grease, oil, efflorescence, paint, or other foreign materials and contaminants. Any solvent cleaning necessary shall meet the recommendations of the coating manufacturer.

Coatings shall be applied in accordance with the manufacturer’s recommendations.

514-001.05 SURFACE PROTECTION. After application(s) of the sealer and/or stain, the concrete surfaces shall be protected as necessary in accordance with the manufacturer’s recommendations.

514-0001.06  ENVIRONMENTAL PROTECTION. During cleaning, surface preparation, and coating operations, the Contractor shall provide appropriate measures (such as suitable protective coverings) to protect the public, the bridge superstructure, work area, river, etc. from cleaning and coating contamination due to drippings, spatter, wind-blown particles, falling objects, etc. The Contractor shall be fully responsible for property damage or personal injury which may result from operations incidental

514-0001.07  METHOD OF MEASUREMENT. The quantity of Anti-Graffiti Coating to be measured for payment will be the number of gallons of material applied in the complete and accepted work, measured to the nearest gallon.

514-0001.08  BASIS OF PAYMENT. The accepted quantity of Anti-Graffiti Coating will be paid for at the Contract unit price per gallon. Payment will be full compensation for furnishing, transporting, handling, and placing the material(s) specified and for furnishing all labor, tools, equipment, and incidentals necessary to complete the work.

Any apparatus, material, and labor not specifically mentioned herein which may be found necessary to complete or perform any portion of the work in a satisfactory manner and in compliance with the requirements implied or intended in these specifications shall be furnished by the Contractor at no additional cost to the Agency.

Payment will be made under:

Pay Item									Pay Item

514.1000001 Anti-Graffiti Coating	Gallon