SECTION 602-0002 – BRICK PAVERS

602-0002.01  DESCRIPTION. This work shall consist of furnishing and placing brick pavers as shown on the Plans and as directed by the Engineer.

The work under this section shall be performed in accordance with these provisions, the Plans, Section 203, Section 301, and Section 541.

602-0002.02  MATERIALS. Materials shall meet the requirements of the following subsections:

Pedestrian Paving Brick	705.01(c)

Mortar, Type II	707.01(c)

(a)	Pavers. Pavers shall be free from seams, cracks, chips, and other structural imperfections or flaws which would impair their structural integrity or appearance, and of a smooth but rustic appearance on at least one upward facing side. Pavers shall be the size and color shown on the Plans, of relatively uniform size and uniform color, matching other existing pavers in the project area if present. Representative samples shall be provided to the Engineer for approval prior to delivery to the required locations on the project.

(b)	Joint Filler for Brick Pavers. Joint filler material for brick and concrete pavers shall be Type II mortar. Prepared color conforming to ASTM C150 shall be added such that the color of the joint filler material matches the color of the surrounding paver.

602-0002.03  CONSTRUCTION REQUIREMENTS.

(a)	Excavation. Excavation shall be made to the required depth and to the width that will permit placing of base and setting beds as shown in the Plans. Excavation shall meet the requirements of Section 203 and shall be paid for under the appropriate excavation item. The wetting of the setting bed course material may be necessary to obtain the required 95% compaction.

(b)	Base. Base shall be placed and compacted in accordance with the requirements of Section 301 and the Plans to an elevation which will result in the top surface of the pavers being flush with the surrounding pavers, concrete, or soil.

(c)	Protection of the Pavers. The pavers shall be stacked at the job site on pallets or suitable platforms that do not obstruct pedestrians or motorists and are protected from damage.

(d)	Installation. Installation shall be performed in accordance with the Plans and the following requirements:

(1)	The depth control base shall be set carefully to bring the pavers, when laid, to proper grade.

(2)	The pavers shall be carefully placed by hand in straight courses with hand tight joints and a uniform top surface. Good alignment shall be kept, and the pattern shall be set in accordance with the Plans. Care shall be taken during the layout to minimize cutting.

(3)	Cutting of the pavers may be necessary to accommodate field conditions and to achieve an accurate and consistent fit. Pavers shall be free from stain, dirt, or dust after cutting. Paver units shall not be cut to a size smaller than one-third of a whole paver.

(4)	No broken pavers shall be used. Cut pavers are not considered broken for these purposes.

(5)	Installation shall be performed in one direction by building forward from previously installed pavers.

(6)	Hand tight joints shall measure from 0 inches to a maximum of 1/8 inch. A dry mixture of the mortar shall be swept over the paver surface. The void shall be filled until the joints are within 1/8-inch of the top surface. The paver surface shall then be lightly fogged with water. Mortar stains that remain shall be cleaned.

(e)	Tolerances. Loose or uneven pavers with greater than a 1/4-inch difference in elevation to the adjacent pavers shall be tamped or removed and reset as required to attain a level surface.

602-0002.04  METHOD OF MEASUREMENT. The quantity of Brick Pavers to be measured for payment will be the number of square feet placed in the complete and accepted work.

602-0002.05  BASIS OF PAYMENT. The accepted quantity of Brick Pavers will be paid for at the contract unit price per square foot. Payment will be full compensation for transporting, handling, and placing the material specified, including subbase, pavers, and mortar; replacing pavers damaged through no fault of the Contractor; cleaning the completed surface as required; and for all labor, materials, tools, equipment, and incidentals necessary to complete the work.

The Contractor shall be responsible for replacing, at no additional cost to the Agency, any pavers that are broken or otherwise damaged by the Contractor’s operations.

Payment will be made under:

Pay Item									Pay Unit

602.2500002  Brick Pavers	Square Foot